Hycrete, Inc.

14 Spielman Road

Fairfield, NJ 07004

Office: (201) 386-8110

Fax: (201) 386-8155

Website:	   www.hycrete.com

SECTION 03 05 12

WATERPROOF CONCRETE CONSTRUCTION

LONG-FORM SPECIFICATION

This long-form specification includes all the details of the concrete quality required for using

Hycrete 360 (Formerly Hycrete System W), which consists of: (1) Hycrete Endure WP (Formerly Hycrete W1000) hydrophobic concrete admixture, a green, high-performing admixture which reduces the absorptivity of concrete; (2) Service during design, preconstruction, and construction; and (3) Performance warranty. An outline version of this specification is also available for insertion into your concrete specification, as long as the concrete quality requirements covered in this specification are included in your concrete specification.

Please note that the service and performance warranty are only available when the application is suitable for membrane-free construction and approved by Hycrete. Please contact Hycrete to ensure that the full system can be available for your project.

For information on Hycrete 360, including performance and applications, please contact Hycrete, Inc. or visit www.hycrete.com.

For best results, display hidden notes to specifier – click on ¶.

This specification is provided to coordinate the use of the Hycrete System W within the project, installed as part or all of the concrete works. The hydrophobic concrete admixture is required to be mixed in with the concrete batch prior to concrete placement.

This section includes products manufactured by Hycrete, Inc.:

Hycrete, Inc.

462 Barell Avenue

Carlstadt, NJ 07072

(201) 386 8110

www.hycrete.com

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

Always check the application and design details with the Hydrophobic Concrete Admixture Manufacturer before designing, bidding, and construction.

PART 1 GENERAL

  - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

  - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

  - SUMMARY

  - This section specifies concrete with Hydrophobic Concrete Admixture and System as indicated on the project drawings for the following:

Revise list below to suit Project.

    - Footings

    - Foundation walls

    - Slabs-on-grade

    - Suspended slabs

    - Water tanks

    - Tunnels

    - Elevator pits

    - (Other-specify)

  - Related sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.  Delete any sections below that are not relevant to this project; add others as required

| 1. | Section 03 15 13 | - | Waterstops |
| --- | --- | --- | --- |
| 2. | Section 03 26 00 | - | Vapor Retarder |
| 3. | Section 03 30 00 | - | Cast-In-Place Concrete |
| 4. | Section 03 38 13 | - | Shotcrete |
| 5. | Section 03 38 00 | - | Post Tensioned Concrete |
| 6. | Section 03 40 00 | - | Precast Concrete |

  - REFERENCES

Delete references from the list below that are not required by the text of the edited section.

  - American Concrete Institute (ACI)

| 1. | ACI 211.1 | - | Standard Practice for Selecting Proportions for Normal, Heavyweight, and Mass Concrete |
| --- | --- | --- | --- |
| 2. | ACI 301 | - | Specifications for Structural Concrete |
| 3. | ACI 302 | - | Guide for Concrete Floor and Slab Construction |
| 4. | ACI 305R | - | Hot Weather Concreting |
| 5. | ACI 306R | - | Cold Weather Concreting |
| 6. | ACI 308 | - | Standard Specification for Curing Concrete |
| 7. | ACI 309R | - | Guide for Consolidation of Concrete |
| 8. | ACI 318 | - | Building Code Requirements for Structural Concrete and Commentary |
| 9. | ACI 357 | - | Guide for the Design and Construction of Fixed Offshore Concrete Structures |

  - American Society for Testing and Materials (ASTM)

| 1. | ASTM A 615 | - | Standard Specification for Deformed and Plain Carbon-Steel Bars for Concrete Reinforcement |
| --- | --- | --- | --- |
| 2. | ASTM A 706 | - | Standard Specification for Low-Alloy Steel Deformed and Plain Bars for Concrete Reinforcement |
| 3. | ASTM A 820 / A 820M | - | Standard Specification for Steel Fibers for Fiber-Reinforced Concrete |
| 4. | ASTM A 996 | - | Standard Specification for Rail-Steel and Axle-Steel Deformed Bars for Concrete Reinforcement |
| 5. | ASTM C 31 / C 31M | - | Standard Practice for Making and Curing Concrete Test Specimens in the Field |
| 6. | ASTM C 33 | - | Standard Specification for Concrete Aggregates |
| 7. | ASTM C 39 / C 39M | - | Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens |
| 8. | ASTM C 94 / C 94M | - | Standard Specification for Ready-Mixed Concrete |
| 9. | ASTM C 138 / C 138 M | - | Standard Test for Density (Unit Weight), Yield, and Air Content (Gravimetric) of Concrete |
| 10. | ASTM C 143 / C 143 M | - | Standard Test Method for Slump of Hydraulic Cement Concrete |
| 11. | ASTM C 150 | - | Standard Specification for Portland Cement |
| 12. | ASTM C 172 | - | Standard Practice for Sampling Freshly Mixed Concrete |
| 13. | ASTM C 173 / C 173 M | - | Standard Test Method for Air Content of Freshly Mixed Concrete by the Volumetric Method |
| 14. | ASTM C 231 | - | Standard Test Method for Air Content of Freshly Mixed Concrete by the Pressure Method |
| 15. | ASTM C 260 | - | Standard Specification for Air-Entraining Admixtures for Concrete |
| 16. | ASTM C 309 | - | Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete |
| 17. | ASTM C 494 / C 494 M | - | Standard Specification for Chemical Admixtures for Concrete |
| 18. | ASTM C 595 | - | Standard Specification for Blended Hydraulic Cements |
| 19. | ASTM C 618 | - | Standard Specification for Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use in Concrete |
| 20. | ASTM C 989 | - | Standard Specification for Ground Granulated Blast-Furnace Slag for Use in Concrete and Mortars |
| 21. | ASTM C 1017 / C 1017M | - | Standard Specification for Chemical Admixtures for Use in Producing Flowing Concrete |
| 22. | ASTM C 1064 / C 1064M | - | Standard Test Method for Temperature of Freshly Mixed Hydraulic-Cement Concrete |
| 23. | ASTM C 1116 / C 1116M | - | Standard Specification for Fiber-Reinforced Concrete |
| 24. | ASTM C 1157 | - | Standard Performance Specification for Hydraulic Cement |
| 25. | ASTM C 1240 | - | Standard Specification for Silica Fume Used in Cementitious Mixtures |
| 26. | ASTM C 1315 | - | Standard Specification for Liquid Membrane-Forming Compounds Having Special Properties for Curing and Sealing Concrete |
| 27. | ASTM C 1602 / C 1602 M | - | Standard Specification for Mixing Water Used in the Production of Hydraulic Cement Concrete |
| 28. | ASTM C 1611 | - | Standard Test Method for Slump Flow of Self-Consolidating Concrete |
| 29. | ASTM E 329 | - | Standard Specification for Agencies Engaged in Construction Inspection and/or Testing |

  - British Standards Institution (BSI)

| 1. | BS 1881-122 | - | Testing Concrete Methods for Determination of Water Absorption |
| --- | --- | --- | --- |

  - SUBMITTALS

  - Submit listed submittals in accordance with the Conditions of the Contract and Division 1 (Submittal Procedures Section).

  - Product Data: Submit Hydrophobic Concrete Admixture Manufacturer’s printed data and instructions for proprietary products and equipment.

  - Shop Drawings:  Submit concrete placement procedures and plan drawings showing locations of isolation joints, contraction (control) joints, and construction joints for slab-on-grade concrete.  Concrete waterproofing-related drawings will be reviewed and approved by the Hydrophobic Concrete Admixture Manufacturer technical personnel before submittal.

  - Quality Assurance/Control Submittals will include:

    - Test Reports:  Upon request, provide test reports from recognized test facilities of material properties and standards compliance.

    - Certificates:  Submit Hydrophobic Concrete Admixture Manufacturer’s certification that the products meet or exceed the specified requirements.

    - Supplier Field Reports:  Include reports of concrete suppliers, field quality-control observations, measurements, and tests.

  - Close-Out Submittals:  Submit the following:

    - Specified warranty documents.

  - QUALITY ASSURANCE

  - Hydrophobic Concrete Admixture Manufacturer Qualifications: Hydrophobic Concrete Admixture Manufacturer will have a minimum of 15 years of experience on projects of similar scope.

  - Manufacturer quality assurance during design, preconstruction and construction:

    - Hydrophobic Concrete Admixture Manufacturer will review and approve the waterproofing details and procedures, including the joint detailing, the waterstop detailing, the reinforcing steel detailing, and all related information.

    - Hydrophobic Concrete Admixture Manufacturer will review and approve the service penetration details prior to installation.

    - Hydrophobic Concrete Admixture Manufacturer will provide pre-placement and placement inspection of hydrophobic concrete production and installation and document specification compliance.

    - Hydrophobic Concrete Admixture Manufacturer will provide pre-placement and placement inspection of waterstop installation and document specification compliance.

  - SLAB OR MEMBER THICKNESS

  - Thickness of slab and other member to provide waterproofing to be as specified and not less than 6 inches. Any slab or other member to provide waterproofing that has a thickness of less than 6 inches to be increased to 6 inches, with design approved by the Engineer.

  - PRE-INSTALLATION CONFERENCE

  - Arrange in compliance with Division 1.

  - Attendance:  Contractor, installer, owner, architect, structural engineer, civil engineer, Hydrophobic Concrete Admixture Manufacturer representative, batch plant representative, and those requested to attend.

  - Meeting Time:  Minimum of 3 weeks prior to the beginning of the work of this Section and work of related Sections affecting the work of this Section.

  - Location:  Project site.

  - Review procedures for conducting work of this Section, including:

    - Review of mix design and mix test results.

    - Mixing procedure.

    - Conditions for acceptance of concrete at project site.

    - Placement procedures.

    - Finishing options and procedures.

    - Curing and crack control procedures.

    - Testing for acceptable moisture emissions, alkalinity pH levels, and relative humidity of concrete slab prior to installation of finish flooring.

    - Affect of the above on the project schedule.

  - DELIVERY, STORAGE, AND HANDLING

  - Conform to provisions of the Section 01 65 10 and the Hydrophobic Concrete Admixture Manufacturer instructions.

  - Mixing and Delivery:  Conform to ASTM C94.

  - Sampling at Delivery:  Conform to ASTM C172.  Cure 4-inch by 8-inch cylinders to provisions of ASTM C31 and compression test compressive strength of cylinders to ASTM C39.

  - Batch Tickets:  Conform to ASTM C94 Option A or C.  Accompany each load, fully executed, and signed.  Log in with inspector at time of entry.  Conform to Source Quality Control requirements specified by this Section.

    - Include water content and water withheld at batch plant.

    - Indicate time to nearest minute that batch was dispatched from plant, when it arrived at site, and when unloading began and was finished.

    - Indicate ambient air temperature and concrete internal temperature at time of arrival.

    - Make written record of water and other additives added to design mix, and the amount of concrete in the truck at the time of addition, after the mix truck left the batch plant.

  - Reject concrete that has reached internal temperature of 89 degrees Fahrenheit or above and when temperature has risen 5 degrees in 10 minutes, indicating concrete is setting up prior to discharge.

  - Store products in accordance with ACI 301.  Do not use admixtures that have been in storage at project site for more than 12 months or which have been subjected to freezing, except as accepted by the Hydrophobic Concrete Admixture Manufacturer and by the structural engineer based on test results.

  - WARRANTY

  - Project Warranty:  Refer to Conditions of the Contract for project warranty provisions.

  - Manufacturer’s Warranty:  Submit, for owner’s acceptance, Hydrophobic Concrete Admixture Manufacturer’s standard warranty document executed by an authorized company official.  Manufacturer’s warranty is in addition to, and not a limitation of, other rights owner may have under the contract documents.

PART 2 PRODUCTS

  - HYDROPHOBIC CONCRETE ADMIXTURE

  - Product generic name: Water-Based Hydrophobic Concrete Admixture for Waterproof Construction plus Service and Performance Warranty.

  - Product name: Hycrete 360 (Formerly Hycrete System W), as manufactured by Hycrete, Inc., 14 Spielman Road, Fairfield, New Jersey, 07004, telephone (201) 386-8110, website hycrete.com.

  - Physical properties

    - Admixture to meet or exceed British Standards Institute (BSI) 1881-122 testing to performance of <1% water absorption.

Verify the warranty type and period with Hydrophobic Concrete Admixture Manufacturer.  Do not specify warranty period and conditions that manufacturer will not honor.

  - Warranty

    - 10-year performance based waterproofing warranty, which covers cost of repair of any leak in protected areas through industry-accepted and approved means.

  - ACCESSORIES

  - Waterstops and Groutable Hose Waterstop System:

    - Waterstops:

      - Shall be placed at all cold joints and penetrations.

b.	Manufacturer and Product: Acceptable to Hydrophobic Concrete Admixture Manufacturer.

    - Groutable hose waterstop systems:

      - Shall be placed at vertical cold joints where required by Hydrophobic Concrete Admixture Manufacturer

b.	Manufacturer and Product: Acceptable to Hydrophobic Concrete Admixture Manufacturer.

  - Concrete Admixtures:

    - Characteristics of all admixtures:

      - Compatible with each other and free of intentionally-added chlorides.

b.	Manufacturer:  Acceptable to Hydrophobic Concrete Admixture Manufacturer.

    - Superplasticizer:

      - Material:  A Superplasticizer to reduce the water requirement of the concrete and to improve the workability for ease in placing and consolidating the concrete.

b.	Material Standard:  ASTM C 494, Type E, Type F, or Type G.

    - Evaporation Retarder:

    - Curing Compound:

      - Hycrete Endure Cure (No Substitutions).

    - Polypropylene Fiber Reinforcement

    - Air-Entraining Admixture:

      - Shall conform to ASTM C 260.

    - Mid-Range Water-Reducing Admixture:

      - Shall conform to ASTM C 494 Type A.

    - High-Range Water-Reducing Admixture:

      - Shall conform to ASTM C 494 Type F or ASTM C 1017 Type I.

    - Accelerating Admixture:

      - Shall conform to ASTM C 494 Type C or E.

    - Retarding Admixture:

      - Shall conform to ASTM C 494 Type B or D.

    - Shrinkage-Reducing Admixture:

    - Alkali-Silica Reaction Inhibiting Admixture:

      - Shall contain a minimum of 30 percent lithium nitrate.

  - MIXES

  - The concrete ready mix supplier must contact the Hydrophobic Concrete Admixture Manufacturer before designing and testing any new mix designs, to receive guidance on achieving proper water absorption characteristics. The concrete ready mix supplier must also report the test results to the Hydrophobic Concrete Admixture Manufacturer. All values must be within the specification limits.

    - All concrete materials used for testing must be same as concrete materials used for construction.

    - Test result requirements for Hydrophobic Concrete in addition to engineer’s performance requirements:  Corrected 30 minute water absorption, age at test 7 days (BS 1881-122):  Not greater than 1.0%

  - Waterproofing System:  All concrete in the locations listed in section 1.02 will be waterproofed by the addition of Hydrophobic Concrete Admixture and additional ingredients including:

    - Hydrophobic Concrete Admixture at the rate of 1.0 U.S. gallon per cubic yard of concrete (5 liters per cubic meter).

    - Superplasticizer at the manufacturer’s recommended rate and appropriate for the placement requirements of the project.

  - Cementitious Content:  The cementitious content of concrete containing Hydrophobic Concrete Admixture will not be less than 550 lbs/yd3 (325 kg/m3) with up to 15% fly ash or 50% slag replacement.

  - Water-Cement Ratio:  0.42 maximum. Water content of Hydrophobic Concrete Admixture and other admixtures to be included in the water-to-cementitious ratio.

Insert Engineer’s performance requirements below:

  - Compressive Strength, 28-day (ASTM C39) - [Specify strength]

  - Air Content (ASTM C173) - [Specify required test method, air content, and tolerance]

  - Slump (ASTM C143) [Specify required slump] or Slump-Flow (ASTM C1611) – [Specify required slump flow]

  - SOURCE QUALITY CONTROL

  - Verification of Performance:  Provide ready-mixed concrete from a concrete supplier approved by the Hydrophobic Concrete Admixture Manufacturer and authorized to dispense the Hydrophobic Concrete Admixture Manufacturer’s waterproofing materials.

PART 3 EXECUTION

  - MANUFACTURER’S INSTRUCTIONS

  - Comply with the Hydrophobic Concrete Admixture Manufacturer’s instructions and recommendations.

  - EXAMINATION

  - Site verification of conditions:

    - Verify that site conditions are acceptable for placement of waterproofed concrete.

    - Utilize Hydrophobic Concrete Admixture Manufacturer’s pre-placement inspection services.

    - Do not proceed with concrete placement until conditions unacceptable to the Hydrophobic Concrete Admixture Manufacturer are corrected.

  - Suitable Condition of Reinforcing Steel:

    - At the time concrete is placed, reinforcement shall be free from mud, oil, or other nonmetallic coatings that decrease bond. Epoxy-coating of steel reinforcement in accordance with standards shall be permitted.

    - Except for prestressing steel, steel reinforcement with rust, mill scale, or a combination of both shall be considered satisfactory, provided the minimum dimensions (including height of deformations) and weight of a hand-wire-brushed test specimen comply with ASTM A 615, ASTM A 706, ASTM A 996.

  - INSTALLATION

  - Waterstops and groutable hose waterstop system components:  Install in accordance with Hydrophobic Concrete Admixture Manufacturer’s recommendations and the drawings.

    - Bentonite waterstops:

      - Shall be placed at all cold joints and penetrations.

- Preparation:

  - Brush off all dust and debris and apply a coat of primer or spray adhesive to the area where the waterstop is to be placed on the standing structural member.

  - Using moderate hand pressure press a continuous bead of waterstop firmly into position on the standing structure. Check to be certain that the waterstop has bonded to the primed area.

  - For proper joining, cut ends with sharp tool at 45 degree angle, and then place ends over one another

  - Peel the protective backing from the exposed side of the waterstop. Knead the overlapped ends together to form continuous, uninterrupted gasket.

  - For shotcrete applications, in addition to the instructions above, utilize masonry nails to hold the waterstop in place on the concrete. Masonry nails should be spaced approximately 12 inches apart. Waterstop must be glued and tied with the use of tie wires to all penetrations.

- Bentonite waterstops must not be installed more than 2 days prior to concrete placement. After installation of waterstops, cover the waterstop with a plastic sheet to protect from weather damage.

- Bentonite waterstops shall be dry and not activated when concrete is placed. If the waterstops have been water damaged shall be replaced before the concrete is placed.

    - Other waterstops and groutable hose waterstop systems:

      - Shall be placed as on drawings and as per Hydrophobic Concrete Admixture Manufacturer’s recommendations.

  - Additional Reinforcement at Re-entrant Angles

    - Where re-entrant angles occur, three #4 or #5 bars spaced at 3 inches OC at least 3 feet long must be placed top and bottom at 90 degrees across all the angles.

  - Concrete:  Place, consolidate, and cure concrete in accordance with ACI 301, ACI 306, ACI 308, and ACI 309.

  - Closure:  Contractor shall allow Hydrophobic Concrete Admixture Manufacturer access to concrete after concrete placement to allow for closure. Hydrophobic Concrete Admixture Manufacturer shall advise Contractor when each area of waterproof concrete is available for finishes.

  - FIELD QUALITY CONTROL

  - Manufacturer’s Field Services:  A representative of the Hydrophobic Concrete Admixture Manufacturer will be present to observe, inspect, and approve the placement of concrete containing Hydrophobic Concrete Admixture Manufacturer’s products.

  - The Contractor shall notify the Hydrophobic Concrete Admixture Manufacturer field representative at least 3 days prior to placement.

  - PROTECTION

  - Protect installed work from damage due to subsequent construction activity on the site.

    - Apply evaporation reducer (ACI 308) on flatwork immediately after finishing, as needed to maintain a film of water on the surface of the finished concrete until the final curing is applied, anytime the evaporation rate exceeds 0.10 lbs/ft2/hr.

    - Apply Hycrete Endure Cure, curing compound immediately to finished or stripped surfaces.

END OF SECTION