Hycrete, Inc.

14 Spielman Road

Fairfield, NJ 07004

Office: (201) 386-8110

Fax: (201) 386-8155

Website:	   www.hycrete.com

SECTION 03 05 00

WATERPROOF AND CORROSION RESISTANT CONCRETE

LONG-FORM SPECIFICATION

This long-form specification includes all the details of the concrete quality required for using

Hycrete Endure CP (Formerly Hycrete X1000) waterproofing and corrosion protection concrete admixture, a green admixture which reduces the absorptivity of concrete and protects steel reinforcement from corrosion. An outline version of this specification is also available for insertion into your concrete specification, as long as the concrete quality requirements covered in this specification are included in your concrete specification.

Please contact Hycrete to ensure that this product is suitable for your project.

For information on Hycrete Endure CP, including performance and applications, please contact Hycrete, Inc. or visit www.hycrete.com.

- For best results, display hidden notes to specifier – click on ¶.

This specification is provided to coordinate the use of Hycrete X1000 within the project, installed as part or all of the concrete works. The waterproofing and corrosion protection concrete admixture is required to be mixed in with the concrete batch prior to concrete placement.

This section includes products manufactured by Hycrete, Inc.:

Hycrete, Inc.

462 Barell Avenue

Carlstadt, NJ 07072

(201) 386 8110

www.hycrete.com

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- PART 1 GENERAL

  - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

  - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

  - SUMMARY

  - This section specifies concrete with Waterproofing and Corrosion Protection Concrete Admixture as indicated on the project drawings for the following:

Revise list below to suit Project.

    - Footings

    - Foundation walls

    - Slabs-on-grade

    - Suspended slabs

    - Water tanks

    - Tunnels

    - Elevator pits

    - Marine structures

    - Bridge structures

    - Containment vessels

    - (Other-specify)

  - Related sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.  Delete any sections below that are not relevant to this project; add others as required

| 1. | Section 03 15 13 | - | Waterstops |
| --- | --- | --- | --- |
| 2. | Section 03 26 00 | - | Vapor Retarder |
| 3. | Section 03 30 00 | - | Cast-In-Place Concrete |
| 4. | Section 03 38 13 | - | Shotcrete |
| 5. | Section 03 38 00 | - | Post Tensioned Concrete |
| 6. | Section 03 40 00 | - | Precast Concrete |

  - REFERENCES

Delete references from the list below that are not required by the text of the edited section.

  - American Concrete Institute (ACI)

| 1. | ACI 211.1 | - | Standard Practice for Selecting Proportions for Normal, Heavyweight, and Mass Concrete |
| --- | --- | --- | --- |
| 2. | ACI 301 | - | Specifications for Structural Concrete |
| 3. | ACI 302 | - | Guide for Concrete Floor and Slab Construction |
| 4. | ACI 305R | - | Hot Weather Concreting |
| 5. | ACI 306R | - | Cold Weather Concreting |
| 6. | ACI 308 | - | Standard Specification for Curing Concrete |
| 7. | ACI 309R | - | Guide for Consolidation of Concrete |
| 8. | ACI 318 | - | Building Code Requirements for Structural Concrete and Commentary |
| 9. | ACI 357 | - | Guide for the Design and Construction of Fixed Offshore Concrete Structures |

  - American Society for Testing and Materials (ASTM)

| 1. | ASTM A 615 | - | Standard Specification for Deformed and Plain Carbon-Steel Bars for Concrete Reinforcement |
| --- | --- | --- | --- |
| 2. | ASTM A 706 | - | Standard Specification for Low-Alloy Steel Deformed and Plain Bars for Concrete Reinforcement |
| 3. | ASTM A 820 / A 820M | - | Standard Specification for Steel Fibers for Fiber-Reinforced Concrete |
| 4. | ASTM A 996 | - | Standard Specification for Rail-Steel and Axle-Steel Deformed Bars for Concrete Reinforcement |
| 5. | ASTM C 31 / C 31M | - | Standard Practice for Making and Curing Concrete Test Specimens in the Field |
| 6. | ASTM C 33 | - | Standard Specification for Concrete Aggregates |
| 7. | ASTM C 39 / C 39M | - | Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens |
| 8. | ASTM C 94 / C 94M | - | Standard Specification for Ready-Mixed Concrete |
| 9. | ASTM C 138 / C 138 M | - | Standard Test for Density (Unit Weight), Yield, and Air Content (Gravimetric) of Concrete |
| 10. | ASTM C 143 / C 143 M | - | Standard Test Method for Slump of Hydraulic Cement Concrete |
| 11. | ASTM C 150 | - | Standard Specification for Portland Cement |
| 12. | ASTM C 172 | - | Standard Practice for Sampling Freshly Mixed Concrete |
| 13. | ASTM C 173 / C 173 M | - | Standard Test Method for Air Content of Freshly Mixed Concrete by the Volumetric Method |
| 14. | ASTM C 231 | - | Standard Test Method for Air Content of Freshly Mixed Concrete by the Pressure Method |
| 15. | ASTM C 260 | - | Standard Specification for Air-Entraining Admixtures for Concrete |
| 16. | ASTM C 309 | - | Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete |
| 17. | ASTM C 494 / C 494 M | - | Standard Specification for Chemical Admixtures for Concrete |
| 18. | ASTM C 595 | - | Standard Specification for Blended Hydraulic Cements |
| 19. | ASTM C 618 | - | Standard Specification for Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use in Concrete |
| 20. | ASTM C 989 | - | Standard Specification for Ground Granulated Blast-Furnace Slag for Use in Concrete and Mortars |
| 21. | ASTM C 1017 / C 1017M | - | Standard Specification for Chemical Admixtures for Use in Producing Flowing Concrete |
| 22. | ASTM C 1064 / C 1064M | - | Standard Test Method for Temperature of Freshly Mixed Hydraulic-Cement Concrete |
| 23. | ASTM C 1116 / C 1116M | - | Standard Specification for Fiber-Reinforced Concrete |
| 24. | ASTM C 1157 | - | Standard Performance Specification for Hydraulic Cement |
| 25. | ASTM C 1240 | - | Standard Specification for Silica Fume Used in Cementitious Mixtures |
| 26. | ASTM C 1315 | - | Standard Specification for Liquid Membrane-Forming Compounds Having Special Properties for Curing and Sealing Concrete |
| 27. | ASTM C 1602 / C 1602 M | - | Standard Specification for Mixing Water Used in the Production of Hydraulic Cement Concrete |
| 28. | ASTM C 1611 | - | Standard Test Method for Slump Flow of Self-Consolidating Concrete |
| 29. | ASTM E 329 | - | Standard Specification for Agencies Engaged in Construction Inspection and/or Testing |
| 30. | ASTM G109 |  | Standard Test Method for Determining Effects of Chemical Admixtures on Corrosion of Embedded Steel Reinforcement in Concrete Exposed to Chloride Environments |
| 31. | ASTM C1585 |  | Standard Test Method for Measurement of Rate of Absorption of Water by Hydraulic-Cement Concretes |

  - British Standards Institution (BSI)

| 1. | BSI 1881-122 | - | Testing Concrete Methods for Determination of Water Absorption |
| --- | --- | --- | --- |

  - SUBMITTALS

  - Submit listed submittals in accordance with the Conditions of the Contract and Division 1 (Submittal Procedures Section).

  - Product Data: Submit Waterproofing and Corrosion Protection Concrete Admixture Manufacturer’s printed data and instructions for proprietary products and equipment.

  - Quality Assurance/Control Submittals will include:

    - Test Reports:  Upon request, provide test reports from recognized test facilities of material properties and standards compliance.

    - Certificates:  Submit Waterproofing and Corrosion Protection Concrete Admixture Manufacturer’s certification that the products meet or exceed the specified requirements.

    - Supplier Field Reports:  Include reports of concrete suppliers, field quality-control observations, measurements, and tests.

  - Close-Out Submittals:  Submit the following:

    - Specified warranty documents.

  - QUALITY ASSURANCE

  - Waterproofing and Corrosion Protection Concrete Admixture Manufacturer Qualifications: Waterproofing and Corrosion Protection Concrete Admixture Manufacturer will have a minimum of 15 years of experience on projects of similar scope.

  - PRE-INSTALLATION CONFERENCE

  - Arrange in compliance with Division 1.

  - Location:  Project site.

  - Review procedures for conducting work of this Section, including:

    - Review of mix design and mix test results.

    - Mixing procedure.

    - Conditions for acceptance of concrete at project site.

    - Placement procedures.

    - Finishing options and procedures.

    - Curing and crack control procedures.

    - Affect of the above on the project schedule.

  - DELIVERY, STORAGE, AND HANDLING

  - Conform to provisions of the Section 01 65 10 and the Waterproof and Corrosion Resistant Concrete Manufacturer instructions.

  - Mixing and Delivery:  Conform to ASTM C94.

  - Sampling at Delivery:  Conform to ASTM C172.  Cure 4-inch by 8-inch cylinders to provisions of ASTM C31 and test compressive strength of cylinders to ASTM C39.

  - Batch Tickets:  Conform to ASTM C94 Option A or C.  Accompany each load, fully executed, and signed.  Log in with inspector at time of entry.  Conform to Source Quality Control requirements specified by this Section.

    - Include water content and water withheld at batch plant.

    - Indicate time to nearest minute that batch was dispatched from plant, when it arrived at site, and when unloading began and was finished.

    - Indicate ambient air temperature and concrete internal temperature at time of arrival.

    - Make written record of water and other additives added to design mix, and the amount of concrete in the truck at the time of addition, after the mix truck left the batch plant.

  - Reject concrete that has reached internal temperature of 89 degrees Fahrenheit or above and when temperature has risen 5 degrees in 10 minutes, indicating concrete is setting up prior to discharge.

  - Store products in accordance with ACI 301.  Do not use admixtures that have been in storage at project site for more than 12 months or which have been subjected to freezing, except as accepted by the Waterproof and Corrosion Resistant Concrete Manufacturer and by the structural engineer based on test results.

  - WARRANTY

  - Project Warranty:  Refer to Conditions of the Contract for project warranty provisions.

  - Manufacturer’s Warranty:  Submit, for owner’s acceptance, Waterproofing and Corrosion Protection Concrete Manufacturer’s standard warranty document executed by an authorized company official.  Manufacturer’s warranty is in addition to, and not a limitation of, other rights owner may have under the contract documents.

- PART 2 PRODUCTS

  - WATERPROOFING AND CORROSION PROTECTION CONCRETE ADMIXTURE

  - Product generic name: Water-Based Waterproofing and Corrosion Protection Concrete Admixture.

  - Product name: Hycrete Endure CP (Formerly Hycrete X1000), as manufactured by Hycrete, Inc., 14 Spielman Road, Fairfield, New Jersey, 07004, telephone (201) 386-8110, website hycrete.com.

  - Physical properties

    - Admixture to meet 50% or greater reduction at seven days according to ASTM C1585.

    - Admixture to meet or exceed British Standards Institute (BSI) 1881-122 testing to performance of <1% water absorption.

    - In chloride-exposed concrete specimens analyzed by chloride depth profiling, admixture to demonstrate a 30% or greater reduction in surface concentration of chlorides (Cs) compared to an untreated control and a diffusion coefficient (D) of 50% or less than the control according to ASTM C1556.

    - Admixture to demonstrate a 75% or greater reduction in rebar iron loss in an uncracked concrete specimen and a 50% or greater reduction in rebar iron loss in a cracked specimen with a pre-formed crack of 0.3mm after four years of testing according to ASTM G109 (Southern Exposure modification:  12 weeks - 4 days wet, 3 days dry, at 100F, then 12 weeks constantly wet).

Verify the warranty type and period with Waterproof and Corrosion Resistant Concrete Admixture Manufacturer.  Do not specify warranty period and conditions that manufacturer will not honor.

  - ACCESSORIES

  - Waterstops (applicable for water-containing structures):

    - Shall be placed at all cold joints and penetrations.

    - Manufacturer and Product: Acceptable to Waterproof Concrete Admixture Manufacturer.

  - Concrete Admixtures:

    - Characteristics of all admixtures:

      - Compatible with each other and free of intentionally-added chlorides.

b.	Manufacturer:  Acceptable to Waterproofing and Corrosion Protection Concrete Admixture Manufacturer.

    - Superplasticizer:

      - Material:  A Superplasticizer to reduce the water requirement of the concrete and to improve the workability for ease in placing and consolidating the concrete.

b.	Material Standard:  Company with ASTM C 494, Type E, Type F, or Type G.

    - Evaporation Retarder:

    - Curing Compound:

      - Hycrete Endure Cure (No Substitution).

    - Polypropylene Fiber Reinforcement

    - Air-Entraining Admixture:

      - Shall conform to ASTM C 260.

    - Mid-Range Water-Reducing Admixture:

      - Shall conform to ASTM C 494 Type A.

    - High-Range Water-Reducing Admixture:

      - Shall conform to ASTM C 494 Type F or ASTM C 1017 Type I.

    - Accelerating Admixture:

      - Shall conform to ASTM C 494 Type C or E.

    - Retarding Admixture:

      - Shall conform to ASTM C 494 Type B or D.

    - Shrinkage-Reducing Admixture:

a.	Shall conform to ASTM C 494

  - MIXES

  - The concrete ready mix supplier must contact the Waterproof and Corrosion Resistant Concrete Admixture Manufacturer before designing and testing any new mix designs, to receive guidance on achieving proper water absorption characteristics. The concrete ready mix supplier must also report the test results to the Waterproof and Corrosion Resistant Concrete Admixture Manufacturer. All values must be within the specification limits.

    - All concrete materials used for testing must be same as concrete materials used for construction.

  - Waterproofing System:  All concrete in the locations listed in section 1.02 will be waterproofed by the addition of Waterproofing and Corrosion Protection Concrete Admixture and additional ingredients including:

    - Waterproofing and Corrosion Protection Concrete Admixture at the rate of 0.5 to 1.25 U.S. gallons per cubic yard of concrete (2 to 5 liters per cubic meter).

    - Superplasticizer at the manufacturer’s recommended rate and appropriate for the placement requirements of the project.

  - Recommended Water-Cement Ratio:  0.45 maximum. Water content of Waterproof Concrete Admixture and other admixtures to be included in the water-to-cementitious ratio.

Insert Engineer’s performance requirements below:

  - Compressive Strength, 28-day (ASTM C39) - [Specify strength]

  - Slump (ASTM C143) [Specify required slump] or Slump-Flow (ASTM C1611) – [Specify required slump flow]

  - SOURCE QUALITY CONTROL

  - Verification of Performance:  Provide ready-mixed concrete from a concrete supplier approved by the Waterproofing and Corrosion Protection Concrete Admixture Manufacturer and authorized to dispense the Waterproofing and Corrosion Protection Concrete Admixture Manufacturer’s waterproofing materials.

- PART 3 EXECUTION

  - MANUFACTURER’S INSTRUCTIONS

  - Comply with the Waterproofing and Corrosion Protection Concrete Admixture Manufacturer’s instructions and recommendations.

  - EXAMINATION

  - Site verification of conditions:

    - Verify that site conditions are acceptable for placement of waterproofed concrete.

    - Do not proceed with concrete placement until conditions unacceptable to the Waterproofing and Corrosion Protection Concrete Admixture Manufacturer are corrected.

  - Suitable Condition of Reinforcing Steel:

    - At the time concrete is placed, reinforcement shall be free from mud, oil, or other nonmetallic coatings that decrease bond. Epoxy-coating of steel reinforcement in accordance with standards shall be permitted.

    - Except for prestressing steel, steel reinforcement with rust, mill scale, or a combination of both shall be considered satisfactory, provided the minimum dimensions (including height of deformations) and weight of a hand-wire-brushed test specimen comply with ASTM A 615, ASTM A 706, ASTM A 996.

  - INSTALLATION

  - Waterstops:

    - Bentonite waterstops:

      - Shall be placed at all cold joints and penetrations.

- Preparation:

  - Brush off all dust and debris and apply a coat of primer or spray adhesive to the area where the waterstop is to be placed on the standing structural member.

  - Using moderate hand pressure press a continuous bead of waterstop firmly into position on the standing structure. Check to be certain that the waterstop has bonded to the primed area.

  - For proper joining, cut ends with sharp tool at 45 degree angle, and then place ends over one another

  - Peel the protective backing from the exposed side of the waterstop. Knead the overlapped ends together to form continuous, uninterrupted gasket.

  - For shotcrete applications, in addition to the instructions above, utilize masonry nails to hold the waterstop in place on the concrete. Masonry nails should be spaced approximately 12 inches apart. Waterstop must be glued and tied with the use of tie wires to all penetrations.

- Bentonite waterstops must not be installed more than 2 days prior to concrete placement. After installation of waterstops, cover the waterstop with a plastic sheet to protect from weather damage.

- Bentonite waterstops shall be dry and not activated when concrete is placed. If the waterstops have been water damaged shall be replaced before the concrete is placed.

    - Other waterstops and groutable hose waterstop systems:

      - Shall be placed as on drawings.

  - Additional Reinforcement at Re-entrant Angles

    - Where re-entrant angles occur, three #4 or #5 bars spaced at 3 inches OC at least 3 feet long must be placed top and bottom at 90 degrees across all the angles.

  - Concrete:  Place, consolidate, and cure concrete in accordance with ACI 301, ACI 306, ACI 308, and ACI 309.

  - PROTECTION

  - Protect installed work from damage due to subsequent construction activity on the site.

    - Apply evaporation reducer (ACI 308) on flatwork immediately after finishing, as needed to maintain a film of water on the surface of the finished concrete until the final curing is applied, anytime the evaporation rate exceeds 0.10 lbs/ft2/hr.

    - Apply Hycrete Endure Cure, curing compound immediately to finished or stripped surfaces.

- END OF SECTION